Degradation of LED chips, encapsulants, reflectors and other components impact LED life in a variety of ways depending on the physical mechanism of each degradation phenomenon. Table 1 describes a set of mathematical models and their combinations  originally identified by Radkov that are used to describe the physical degradation phenomena of LED components and products.  In the absence of other LED lumen depreciation estimation methods, our statistical analysis used this set of models for exploration and study toward a structured industry acceptable LED life estimation method.

| # | Parameters |  |  | Decay Rate | Closed Form Solution | Degradation Mechanism |
| --- | --- | --- | --- | --- | --- | --- |
|  | k3 | k2 | k1 |  |  |  |
| 0 | 0 | 0 | 0 | dIv/dt = 0 | Iv = Iv0 | None observed |
| 1 | 0 | 0 | 1 | dIv/dt = k1 | Iv = Iv0 +k1(t-t0) | Drift of charged defects in chip |
| 2 | 0 | 1 | 0 | dIv/dt = k2Iv | Iv = Iv0 exp[(k2(t-t0)] | Thermal decomposition of encapsulant |
| 3 | 0 | 1 | 1 | dIv/dt = k1 + k2Iv | Iv = (Iv0+k1/k2) exp[k2(t-t0)] -k1/k2 | Model 1+ Model 2 |
| 4 | 1 | 0 | 0 | dIv/dt = k3/t | Iv = Iv0 +k3 ln(t/t0) | Corrosion of reflector |
| 5 | 1 | 0 | 1 | dIv/dt = k1 + k3/t | Iv = Iv0 +k1(t-t0) +k3 ln(t/t0) | Model 1+Model 4 |

Table 1 Engineering-based models for describing degradation mechanisms of various LED components and products